## Slide 1
DUŠAN BEREK, IVAN NOVÁK,
POLYMER INSTITUTE, SLOVAK ACADEMY OF SCIENCES
84541 BRATISLAVA, SLOVAKIA
DAVID HUNKELER, AQUATECH-WATER, GENEVA, SWITZERLAND
HLUBOČEPY 2019
Removal of ions of
harmful metals from
water with help of
original composite sorbent

## Slide 2
THE PRIMARY TASK – PREPARATION
INEXPENSIVE
POROUS CARBON FIBERS
WITH ADJUSTABLE PROPERTIES
AND BROAD APPLICABILITY - BY
CARBONIZATION OF CELLULOSE

## Slide 3
CELLULOSE 
CARBONIZATION 
PYROLYTIC CARBON 
 POROUS CARBON FIBERS

## Slide 4
WHY FIBERS?
BECAUSE
 CELLULOSE USUALLY
APPEARS IN FORM OF FIBERS OR FIBER-LIKE STRUCTURE
 COMPARED TO PARTICULATE MATERIALS - FIBERS ARE EASIER TO MANIPULATE AND THEIR BED EXHIBITS DECREASED RESISTANCE TO FLOW OF GASES AND LIQUIDS

## Slide 5
MACROSCOPIC PROPERTIES OF C-FIBERS
BOTH LENGTH AND DIAMETER ARE DETERMINED BY STARTING MATERIAL:
 INDUSTRIAL RAW CELLULOSE
 INDUSTRIAL DELIGNIFIED CELLULOSE –
PULP, COTTON WOOL
 NATIVE RAW CELLULOSIC MATERIALS –
YUTA, SISAL, (CRUSHED) BAMBOO,
OIL- AND COCO-PALMS, SAW-DUST....
 CRUSHED WASTE PAPER
 CELLULOSE NANOFIBERS SOON COME UNDER STUDY

## Slide 6
INDUSTRIAL DELIGNIFIED CELLULOSE
„GREENCEL“, HUNCOVCE, SLOVAKIA

## Slide 7
GENERATION OF PORES
ACTION OF ACTIVATORS, POROGENS
 MAINLY Zn SALTS, P AND B SUBSTANCES
 ALTERNATIVES: Si, Ti, etc.
PROBLEMS: PRICE AND ECOLOGY
CHALLENGE  CARBONIZATION
WITHOUT POROGENS
HLUBOČEPY 2019

## Slide 8
CARBONIZATION UNDER NITROGEN
EXPENSIVE
SOPHISTICATED REACTORS
SIMPLE APPROACH IS NEEDED FOR
PRACTICAL APPLICATION
CLOSED VESSELS WITH
PROTECTIVE ATMOSPHERE
OF CO2
HLUBOČEPY 2019

## Slide 9
BASIC PHYSICAL PROPERTIES OF
SO FAR PREPARED MICROPOROUS
CARBON FIBERS:
-- LENGTH FROM 20 µm TO SEVERAL cm
-- DIAMETER FROM 1 to 100 µm
B.E.T. SURFACE AREA FROM FEW m2.g-1 to ALMOST 2,500 (!) m2.g-1
HLUBOČEPY 2019

## Slide 10
PORE STRUCTURE OF MICRO-POROUS CARBON FIBERS
positron annihilation lifetime spectroscopy
b.e.t. argon adsorption isothermS and gel permeation chromatography -- indicate presence of
narrow pores with similar size in the range of 0.6 nm

## Slide 12
CURRENT ASSUMPTION -
 RATHER UNIFORM, DEEP NANO-PORES
WITH ORIFICES OF DIFFERENT SIZE,
SHAPE AND VOLUME
HLUBOČEPY 2019

## Slide 13
FORMATION OF COMPOSITES
 DEPOSITION OF NANO- AND MICROPARTICLES OF ACTIVE SUBSTANCE EXCLUSIVELY ON THE SURFACE OF MICROPOROUS CARBON FIBERS
 ORIGINALLY STRUCTURED COMPOSITE MATERIALS
HLUBOČEPY 2019

## Slide 14
PRINCIPLE --
PORES OF SUBSTRATE MUST BE SMALL ENOUGH TO PREVENT PENETRATION OF PRECURORS OF ACTIVE SUBSTANCE, FeCl3, Ag(NO3), ZnCl2, etc.
THE ACTIVE SUBSTANCE GENERATED FROM PRECURSOR BY PRECIPITATION IS DEPOSITED EXCLUSIVELY ON THE SURFACE OF CARRIER SUBSTRATE –
---- MICROPOROUS CARBON FIBERS

## Slide 15
FEATURES OF COMPOSITES
 LARGE AND EASILY
ACCESSIBLE SURFACE
OF ACTIVE SUBSTANCE
 LOW FLOW RESISTANCE

## Slide 16
HYDRATED FERRIC HYDROXIDE
IS KNOWN FOR ITS HIGH AFFINITY
TO NUMEROUS METAL IONS, incl.
HARMFUL As, Sb, Cr, Pb, Se, ...
NANO- AND MICROPARTICLES OF
Fe(OH)3.n(H2O) WERE DEPOSITED
ON THE MICROPOROUS CARBON
FIBER SURFACE – „CF-Fe“

## Slide 18
C-FIBER WITH DEPOSITED
HYDRATED FERRIC HYDROXIDE

## Slide 19
BOTH EFFICIENCY & CAPACITY OF
CF-Fe COMPOSITE ADSORBENTS
FOR REMOVAL OF HARMFUL
METALS FROM WATER WERE
TESTED UNDER STATIC AND ALSO
DYNAMIC (FLOW-THROUGH)
CONDITIONS
HUSTOPEČE 2019

## Slide 20
Chart: Efficiency of trapping As from spiked water, c(As) = 914,0 µg/l
| č.158-SAV | č.159-SAV | č.161-SAV | č.162-SAV | č.165-SAV | č.166-SAV | GEH
 | 92.64 | 97.8 | 95.95 | 97.6 | 76.7 | 94.4 | 37.09

## Slide 21
Chart: Efficiency of trapping Sb from spiked water, c(Sb) = 65,2 µg/l
| č.158-SAV | č.159-SAV | č.161-SAV | č.162-SAV | č.165-SAV | č.166-SAV | GEH
 | 83.27 | 84.87 | 84.27 | 84.67 | 79.73 | 81.13 | 59.87
SAMPLE NUMBER GEH
145 146 148 151 153 157

## Slide 22
CONCLUSION 
COMPOSITES CF-Fe EXHIBIT HIGH
ADSORPTION EFFICIENCY AND CAPACITY
FOR As, Sb, Pb, Cd, Se, Cr and Ni, as well
as natural and synthetic RADIONUCLIDES
SUITABILITY FOR WATER TREATMENT
AND PURIFICATION

## Slide 23
A SPECIFIC FEATURE OF
COMPOSITE SORBENT WITH A
CARBON CARRIER
TWO DISTINCT KINDS OF SURFACES
ARE PRESENT
 SURFACE OF NANOPARTICLES
 SURFACE OF ORIGINAL CARBON

## Slide 24
NUMEROUS ORGANIC IMPURITIES FROM
WATER AND GASES CAN BE REMOVED
WITH HELP OF COMPOSITE MATERIALS
 WASTE OF BOTH SYNTHESES AND
INDUSTRIAL PRODUCTION INCLUDING
COLORANTS, etc.
 MUNICIPAL AND AGRICULTURAL
SEWAGE INVOLVING DETERGENTS,
NITRATES, PRODUCTS OF DIGESTION,
etc., etc.

## Slide 25
FURTHER POSSIBLE APPLICATIONS OF
COMPOSITES BASED ON CARBON FIBERS:
 SORBENTS
-- FOR PURIFICATION OF GASES AND LIQUIDS -- PRODUCTS OF INDUSTRIAL CHEMICAL SYNTHESES
-- FOR SELECTIVE ENTRAPMENT AND SEQUESTRATION OF GASES
 CATALYSTS

## Slide 26
NUMEROUS OTHER APPLICATIONS
OF MICROPOROUS CARBON FIBERS
ARE AT HAND
A ROOM FOR COOPERATION WITH
MANY PARTNERS IS AVAILABLE
 EVERYONE IS WELCOME
CONTACT:
dusan.berek@savba.sk
HLUBOČEPY 2019