## Slide 1: MiscanValue - Creating value chains for utilization of miscanthus fibres from sustainably managed marginal and post-mining areas
Dr. Martin Zahel, Manuela Fiedler
Head of Business Division Fibres & Composites
Laboratory & Project Manager Fibres & Composites
Paper and packaging products from miscanthus
21.09.2022

## Slide 2: Virgin and Secondary Fibres for Paper Production
Chemical Pulping Secondary Fibres:
Mechanical Pulping
Alternative Fibre Sources Papermaking
Pulping
Bleach-ing
Bleach-ing
SGW TMP CTMP APTMP
Wood
Wood
Stock Prepa-ration
Paper-machine
Coating
Recycling
Usage
Process-ing
Paper
Plants
Individual Pretreatment and Processing Spets

## Slide 3: Pulping vs. Properties
Intensity of Pulping
Strength
Lignin Content
Bending Stiffness
Volume
Biomass
RMP
TMP
CTMP
BCTMP
mech.
Pulping
mech. & chem.
Pulping
Bleaching
Pulp
Bleached
Pulp
Bleaching
chem.
Pulping
Dewatering

## Slide 4: Miscanthus Fibres for Papermaking?
Investigation of mechanical and chemical Pulping Technologies:
  TMP-Refining and Acetosolv-Pulping
Measuring the Fibre Properties
  Lignin Content, Charge Properties, Degree of Polymerization, Fibre Morphology and Water Retention Value
Generation and Testing of Laboratory Paper Materials
  Tensile and Tear Strength

## Slide 5
Miscanthus Fibre properties

## Slide 6: Chemical properties
Fibres from the acetosolv pulping have a significantly lower GVZ (limiting viscosity number) than the fibres from the sulphate digestion.
The total charge of the fibrous materials from acetosolv digestion is many times higher than the fibrous materials from sulphate digestion
sample | Lignin % | GVZ ml/g | Total charge mmol/kg | Surface charge µeq/g
TMP | - | 395 | - | -
CTMP V III | - | - | - | -
Acetosolv 1 | 8,0 | 263 | 65,2 | -195,6
Acetosolv 2 | 13,2 | 263 | 59,3 | -204,4
Acetosolv 3 | 15,9 | 208 | 43,7 | -191,6
Acetosolv 4 | 1,4 | 317 | 65,2 | -104,7
Sulphate pulp spruce/pine | <1 | 730 | 22,2 | - 54,1
Sulfat pulp eucalyptus | < 1 | 743 | 25,7 | - 71,2
Reference Wood Pulps: Datasheet values

## Slide 7: Fiber length vs Water retenention value WRV
Miscanthus pulps have short fibres, lots of fines -> a high specific surface area -> high WRV.
Sulphate pulps have significantly lower WRV values

## Slide 8: Drainage resistance SR – PFI Mill
the Miscanthus CTMP develops very high SR values when ground -> fines content increases
the pulps produced by the sulphate process are more resistant to grinding than the Miscanthus pulps

## Slide 9
Paper properties

## Slide 10: Laboratory Sheet Forming: Rapid Koethen
Pressing
Sheet before Drying
Sheet Forming
Dewatering

## Slide 11: Handsheets
Acetosolv
CTMP
M2 + TMP

## Slide 12: Tensile-Index – PFI Mill
the Tensile Index of the Acetosolv pulps (unrefined) is significantly higher than the pulps produced after sulphate digestion (unrefined)

## Slide 13: Tear-Index – PFI Mill
the tear index of the sulphate fibre spruce/pine is the highest
the Miscanthus fibres have a lower tear index which is only slightly changed by grinding.

## Slide 14: Next Steps: Preparing Paper at a Pilot Paper Machine
How do Miscanthus pulps behave towards additives?
In which paper grades could these fibres be used?

## Slide 15: Summary
Miscanthus fibres have a higher total and surface charge than the sulphate fibres.
the Miscanthus fibres were not bleached -> higher lignin content
Miscanthus acetosolv pulps, unground, achieve significantly higher strength (Tensile Index) than pulps produced after sulphate digestion.
Low GVZ of Miscanthus Acetosolv fibres -> higher strength than sulphate fibres
IGF CORNET 283 EBR
Dr. Martin Zahel
T 03529-551-674
M 0176-12146-350
E martin.zahel@ptspaper.de
Head of Business Division
Fibres & Composites